## Slide 1: Quantum Dots
Stephen Kelly

## Slide 2: History
First discovered around 1982 by Alexey Ekimov
Term was coined in 1986
Also called “Artificial Atoms”
Notes: Russian ad

## Slide 4
Image credit: http://www.photonics.com/images/spectra/features/2007/May/QuantumDots_Fig5_CoreShell.jpg

## Slide 5: Properties
Relatively precise control of photon emission/absorption wavelength
  Smaller R -> smaller wavelength, and vice versa
Formed via colloidal synthesis
  Inkjet and spincoating
  Low cost
High quantum yield or “one-for-two” exchange

## Slide 6: Materials
Cadmium Sulfide (CdS)
Cadmium Telleride (CdTe)
Lead Sulfide (PbS)
Copper Indium Sulfide (CuInS2)
Gold Indium Sulfide (AgInS2)
Zinc Sulfide (ZnS)

## Slide 8: One-Pot Synthesis
Kango, Sarita & Kalia, Susheel & Thakur, Pankaj & Kumari, Bandna & Pathania, Deepak. (2014). Semiconductor–Polymer Hybrid Materials. 10.1007/12_2014_295.
Notes: Trioctylphosphine oxide (TOPO) is an organophosphorus compound with the formula OP(C8H17)3. Frequently referred to as TOPO, this compound is used as an extraction or stabilizing agent. It is an air-stable white solid at room temperature.
Need stabilizing agents, otherwise it is like solder wetting

## Slide 9: Synthesis Benefits
Still based on growing crystals
Purity is governed by reagent quantity
Temperatures govern growth rates

## Slide 10: Applications

## Slide 12
Nanosys Inc.

## Slide 13
Luminescence spectra of CdTe quantum dots of different sizes from ca. 1 nm (left curve) to ca. 7 nm (green curve)

## Slide 14
Shin-Tson Wu, University of Central Florida

## Slide 15: Comparison to LED Binning

## Slide 16
LED Binning

## Slide 17
Notes: Flux – Amount of light output
Color – Frequency of Light
Vf – applied voltage

## Slide 18: LED Binning
Crystal growth is inconsistent
Doping locations are not controlled
Efficiency is sacrificed in certain color ranges

## Slide 19: Quantum dots allows for improved precision, efficiency and output gamut

## Slide 20
Marc Achermann - Los Alamos National Laboratory, http://www.sandia.gov/news-center/news-releases/2004/micro-nano/well.html
Quantum Dot Laser

## Slide 21: Solar Applications

## Slide 22: Shockley–Queisser limit

## Slide 25
Lukasz Brzozowski - Lukasz Brzozowski, Director, Photovoltaics Research Program, Department of Electrical and Computer Engineering, University of Toronto

## Slide 26: Biological

## Slide 27: Immunohistochemistry

## Slide 28: Physical Analysis

## Slide 29: Particle in a Box

## Slide 30: Brus Equation
  Egap (CdSe) = 1.74 eV = 2.8·10−19 Joules,
  me* (CdSe) = 0.13 me = 1.18·10−31 kg,
  mh* (CdSe) = 0.45 me = 4.09·10−31 kg.
  h = plancks constant (6.62607004 × 10-34 m2 kg / s)
  r = radius of QD
Notes: The Brus equation[1] can be used to describe the emission energy of quantum dot semiconductor nanocrystals (such as CdSe nanocrystals) in terms of the band gap energy Egap, Planck's constant h, the radius of the quantum dot r, as well as the effective mass of the excited electron me* and of the excited hole mh*.
The radius of the quantum dot affects the wavelength of the emitted light due to quantum confinement, and this equation describes the effect of changing the radius of the quantum dot on the wavelength λ of the emitted light (and thereby on the emission energy ΔE = hc/λ, where c is the speed of light). This is useful for calculating the radius of a quantum dot from experimentally determined parameters.
The overall equation is[2]
Egap, me*, and mh* are unique for each nanocrystal composition. For example, with CdSe nanocrystals:
  Egap (CdSe) = 1.74 eV = 2.8·10−19 Joules,
  me* (CdSe) = 0.13 me = 1.18·10−31 kg,
  mh* (CdSe) = 0.45 me = 4.09·10−31 kg.
E= h c/lambda

## Slide 31
Brus, Louis. “Electronic Wave Functions in Semiconductor Clusters: Experiment and Theory.” The Journal of Physical Chemistry 90, no. 12 (June 1986): 2555–60. https://doi.org/10.1021/j100403a003.

## Slide 32: Bloch Wave

## Slide 33: Block Wave

## Slide 34: Evanescent Waves

## Slide 35: Evanescent Waves (Quantum Tunneling)
Felix Kling

## Slide 37: Multiple Exciton Generation

## Slide 38: Quantum Yield
Notes: To improve fluorescence quantum yield, quantum dots can be made with "shells" of a larger bandgap semiconductor material around them.
TU Dresden:
are 0.65−0.85 for CdSe,(29, 30) 0.1−0.4 for InP,(31-33) and 0.30−0.75 for CdTe and CdHgTe(34-36) as well as 0.26−0.70 and 0.1−0.8 for the NIR emitters PbS(37, 38) and PbSe, respectively.(39, 40)

## Slide 39: Applications
Displays
Lasers
Photodetectors
Immunohistochemistry (Biomarkers)
Solar?

## Slide 40: Future Challenges
Alternative Materials (EHS)
Tabulate band gaps
Measure/compute effective electron mass

## Slide 41: References
Iafrate, G. J., K. Hess, J. B. Krieger, and M. Macucci. “Capacitive Nature of Atomic-Sized Structures.” Physical Review B 52, no. 15 (October 15, 1995): 10737–39. https://doi.org/10.1103/PhysRevB.52.10737.
Brus, Louis. “Chemistry and Physics of Semiconductor Nanocrystals,” n.d., 33.
Brus, Louis. “Electronic Wave Functions in Semiconductor Clusters: Experiment and Theory.” The Journal of Physical Chemistry 90, no. 12 (June 1986): 2555–60. https://doi.org/10.1021/j100403a003.
Kippeny, Tadd, Laura A. Swafford, and Sandra J. Rosenthal. “Semiconductor Nanocrystals: A Powerful Visual Aid for Introducing the Particle in a Box.” Journal of Chemical Education 79, no. 9 (September 2002): 1094. https://doi.org/10.1021/ed079p1094.

## Slide 42: References
Pathak, Smita, Elizabeth Cao, Marie C. Davidson, Sungho Jin, and Gabriel A. Silva. “Quantum Dot Applications to Neuroscience: New Tools for Probing Neurons and Glia.” Journal of Neuroscience 26, no. 7 (February 15, 2006): 1893–95. https://doi.org/10.1523/JNEUROSCI.3847-05.2006.
Rühle, Sven. “Tabulated Values of the Shockley–Queisser Limit for Single Junction Solar Cells.” Solar Energy 130 (June 2016): 139–47. https://doi.org/10.1016/j.solener.2016.02.015.
Gilmore, Rachel H., Samuel W. Winslow, Elizabeth M. Y. Lee, Matthew Nickol Ashner, Kevin G. Yager, Adam P. Willard, and William A. Tisdale. “Inverse Temperature Dependence of Charge Carrier Hopping in Quantum Dot Solids.” ACS Nano 12, no. 8 (August 28, 2018): 7741–49. https://doi.org/10.1021/acsnano.8b01643.